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The colour of the new mortar, which should match the original mortar before weathering,
should be provided by the use of a well graded sharp sand.

The mortar will be gauged 3-1 sand - lime and the lime to be NHL 3.5,
Gauge boxes must be used.

joints should be carefully raked out manually to a depth of at least 25mm and up to 40mm,
depending upon the width of the joint, and flushed out with clean water. Cutting out of
existing mortar with mechanical discs s not acceptable.

All joints maust be dampened prior to placing the mortar
Any joints over a depth of 40mm should be back pointed and tamped in where necessary.

The joints should be solidly filled with new mortar and finished slightly proud. After the
nital set has taken place the joint should be knocked back with a bristle brush to expose both
he aggregate and the edges of the adjacent stone. The joints can be picked over to give
movement to the finish.

Where existing stone is generally eroded, the face of the mortar should be kept back to the
point at which the joint remains the original width. Re pointing should not increase the width
of the original joints

Al work must be properly protected with hessian during and afier the works.




